Shape analysis of  carbon nanotube junctions

Ante Graovaca,b ,  István Lászlóc and Tomaž Pisanskid

aDepartment of Chemistry, Faculty of Science, University of Split, Nikole Tesle 12, HR-21000 Split, Croatia

bDepartment of Physical Chemistry, Ruđer Bošković Institute,

P. O. Box 180,  HR-10002 Zagreb,  Croatia

cDepartment of Theoretical Physics, Institute of Physics,  Budapest University of Technology and Economics, H-1521  Budapest, Hungary

dDepartment of Theorettical Computer Science Institute of Mathematics, Physics and Mechanics, University of Ljubljana, SL-1000 Ljubljana, Jadranska 19, Slovenia

Abstract.  Using the eigenvectors of the Laplacian matrix of the graph describing the topology of a  nanotube junction we have developed a shape analysis. The X, Y, Z relaxed Descartes coordinates of the atoms were calculated as a linear combination of the eigenvectors. We have obtained that the partial sums generated thre-dimensional structures only if they contained all the three bi-lobal eigenvectors of the Laplacian. We have found partial sums that produced satisfactory initial coordinates for molecular mechanics calculations.

Introduction

There are several theoretical propositions for various carbon nanotube junctions[1-21] and in most  of the cases the position of the atoms are given with the help of a molecular mechanics procedure. It was found, however,  that some eigenvectors of the adjacency matrix can produce satisfactory Descartes coordinates for several spherical, toroidal and planar structures [22-31]. In these procedures usually it is supposed that the molecules under study are in two or in three dimension spherical. Namely for fullerenes the spheres are good approximations and the tori can be imagined as the direct product of two circles. The topological coordinates of nanotubes and planar structures are developed from the correspondent topological coordinates of tori. The question arrives whether the method of the topological coordinates  can be used for non-spherical structures as well? Here we shall present a shape analysis of nanotube junctions in order to examine to possibilities to extend the topological coordinate method to non-spherical structures.

Topological coordinates

We describe the atomic arrangement of a molecule by the graph  where  is the set of vertices and is  that of the edges. Let  be the adjacency matrix of  graph  of n vertices. The vertices  i, j are understood to be adjacent iff . For non-adjacent vertices  .   The vertices correspond to the carbon atoms and the edges to the first neighbour bonds. Let the diagonal matrix  be given by , where  is the degree of a vertex .  The Laplacian matrix will be defined as . This definition of  correspond to the usual definition of the Laplacian if it is multiplied by -1. Using our definition the ordering of the eigenvectors of the adjacency matrix and the Laplacian is the same. With the help of the adjacency matrix  and the Laplacian matrix we can describe the topological structure  but for further investigation usually we need the Cartesian coordinates of the atoms as well. A simple solution to this problem is the topological coordinate method proposed  by  Fowler and Manolopoulos [22 ] and by Pisanski and Shawe-Taylor [23].   The topological coordinate method is based on the so called bi-lobal eigenvectors of the adjacency matrix  [22-25]. Eigenvectors having this bi-lobal property can be identified by the graph-disconnection test [26]: for a candidate eigenvector, colour all vertices  of  bearing positive coefficients black, all bearing negative coefficients white, and all bearing a zero coefficient grey; now delete all grey vertices, all edges connecting a black to a white vertex; if the graph now consists of exactly two connected components, one of black and  one of white vertices, then the eigenvector is of bi-lobal. If the number of connected uncoloured subsets is greater than two we call the correspondent eigenvector  multi-lobal.

We arrange in descending order the   eigenvalues   of the adjacency matrix    as:

(1)

where  is the eigenvector with eigenvalue  . In the case of structures homeomorphic to the sphere, like the fullerenes, the first three bi-lobal eigenvectors , ,  and determine the  topological coordinates of the i-th atom by the relations:

(2)

(3)

(4)

with the scaling factors  or . The most realistic picture of  fullerenes can be found by the scaling factor  [22,27]

.                                                               (5).

In the following years the topological coordinate method was extended to tori [26,28,29], nanotubes[27,29] and planar[30,31] structures.

The graph of a  nanotube junctions

Introducing two unit vectors  and    on the graphene sheet and two integers  and  we can assign coordinates  to each hexagon of the sheet [32].

Hexagonal nanotubes are obtained by rolling up a rectangle defined by  the chiral vector

(6)

and the multiple of the translation vector

(7)

where          and          are integers and  is the highest common divisor of , with  if  is not a multiple of . During the rolling up procedure the sides parallel with the translation vector  are identified [32].

Let us suppose that we want to calculate the topological coordinates of a junction made of three open ended nanotubes with  parameters    ,   and . We suppose further that the topological structure of the junction is constructed with some algorithm as for example of references [1-21]. That is we know the graph  of the junction. In our special case  for the number of vertices and edges we have in order  and .

The atomic coordinates are in Angstroms and the interatomic distances are about Å.

Shape analysis of nanotube junctions

Although nanotube junctions are  homeomorphic to the sphere the eigenvectors of the adjacency matrix  yields improper topological coordinates by applying  Eqs (1-5).

There are two problems with the obtained  structures. The first one is that the ends of the nanotubes turne back and the second problem is that they became narrower as one move to their tips. We could eliminate the first problem by replacing the  adjacency matrix  by the Laplacian .  In order to find information for solving the second problem too, we developed a shape analysis method based on the eigenvectors of the Laplacian.

Let us suppose that we have the exact  coordinates of the atoms in the nanotube junction. In this case   X, Y and Z   are n-dimensional vectors containing the x, y and z coordinates of the atoms in order.  We suppose  that the centre of mass of the molecule is in the origin and the molecule is directed in such a way that the eigenvectors of its tensor of inertia are showing to the directions of the x, y and z axis.

Using the following scalar products

,   and                                                        (10)

the atomic coordinates can be written as

,      and     .                                        (11)

Here    is the eigenvector of the Laplacian  and the corresponding eigenvectors   are ordered in descending order as in Eq. (1). We say that the weight of the eigenvector   in

X  is . We use similar notation for  and  as well, concerning the weight of  in Y and Z.

Table 1. shows the calculated ,  and   coefficients for our structure under study.

The junction of three nanotubes  ,   and  contains  vertices and  edges and  the atomic coordinates are in Angstroms with interatomic distances  about Å.

The  lobality of the 50 highest eigenvalues of the Laplacian are shown in Table 2.

Let  we introduce the notations

,    and              (12)

and

,      .                                (13)

The convergence of the structure can be quantified with the following parameters:

(14)

(15)

(16)

(17)

Table 3. shows these parameters calculated for the nanotube junction.

Table 1. The   ,   and   coefficients in the function of the k<51 eigenvectors of the graph  under study.       _________________________________________________________________

__________________________________________________________________

1.0000000          0.0000000          0.0000000          0.0000000

2.0000000        531.5254607         13.3827301          0.6325792

3.0000000        -16.2079966        430.8542357          0.0952077

4.0000000          3.5449696        -13.0315564         -5.4410281

5.0000000         42.4655249         -2.8137039         -9.6967041

6.0000000          2.0122291         27.8030055         -4.3774035

7.0000000          1.4159249         -2.0932022       -116.3577655

8.0000000          3.1082390        -70.5642098          9.2422098

9.0000000        -50.0196729         18.0156682          4.3182771

10.0000000         25.0383045          9.8005451          5.8380187

11.0000000        -51.9100731         -6.4189166         -2.6698094

12.0000000         -6.9409825        -32.8224709          4.6656589

13.0000000         -9.9775458        -26.2444492        -12.8144739

14.0000000          0.9532447          1.4957518         39.5057271

15.0000000         14.5111931          1.2285586          2.3931973

16.0000000         -0.4005245        -24.0277980          0.3733706

17.0000000         -1.4364734         -0.6421640         -4.8800356

18.0000000          0.0620605         -2.1570805          2.0228203

19.0000000         -0.0290088         -0.3082656          5.7207245

20.0000000         -0.2273765          1.4636923         -0.4286804

21.0000000         -0.4610300          2.8193019          0.7213372

22.0000000         -0.6741517         -0.4142709         -9.9134401

23.0000000          1.3758623          5.7961101         -1.3705850

24.0000000          7.7266471         -0.3504044         -0.2477901

25.0000000          1.2064242          0.3481832          0.6712200

26.0000000          1.3092264          1.7305266          0.1196681

27.0000000         -2.7900128          0.6966942          3.4279522

28.0000000          7.1753631         -0.6887413          0.5888154

29.0000000         -8.0446988         -1.7900420          0.3661587

30.0000000          1.2894355         -6.3156190          1.1002530

31.0000000         -0.3864592          2.2830875          1.3178089

32.0000000          0.6409442         -3.7831982          0.0234788

33.0000000         -0.5764697          0.3262168         -0.8595379

34.0000000         -0.3170529          0.6797819         -0.1916831

35.0000000          1.4448802         -0.6699093         -0.1544033

36.0000000          0.9119649         -0.0569799         -0.0253382

37.0000000          0.2992687         -1.8880457         -0.1531114

38.0000000         -0.3627125         -2.3280220          0.1244858

39.0000000         -1.3245159         -3.0818850         -0.5704134

40.0000000         -0.4764249          1.5540824          0.3039358

41.0000000          0.0157165         -1.7605137          0.5028698

42.0000000          0.3260193          0.3057477          2.3832007

43.0000000          0.2710680          1.1237566          0.2571330

44.0000000          1.5680830          0.0820025          0.5416591

45.0000000          1.5472688          0.3921164         -0.0685210

46.0000000          0.5837059         -0.8025218          0.2729327

47.0000000          1.7244431         -0.2540253         -0.2961865

48.0000000          1.0151762         -1.2792596          0.8287651

49.0000000          0.1709302          0.9799888         -0.0133521

50.0000000         -0.0072069         -0.0782976         -0.5005451

_____________________________________________________________________

___________________________________________________________________

Table 2.  The number of negative, zero and positive lobes in order #(-), #(0) and #(+) for the    eigenvectors of the Laplacian  (k<51).

_________________________________________________

k          Number of sets                            Eigenvalues

__________________

#(-)     #(0)      #(+)

______________________________________

1    0    0    1          0.0000000

2    1    0    1         -0.0031599

3    1    0    1         -0.0039442

4    1    0    3         -0.0148721

5    2    0    2         -0.0279367

6    2    0    3         -0.0345535

7    1    0    1         -0.0514583

8    3    0    1         -0.0551314

9    1    0    2         -0.0568913

10    2    0    1         -0.0577398

11    2    0    2         -0.0590989

12    3    0    2         -0.0596147

13    3    0    2         -0.0605058

14    1    0    2         -0.0647244

15    4    0    3         -0.0711096

16    3    0    3         -0.0741113

17    3    0    2         -0.0829832

18    2    0    3         -0.0862043

19    2    0    4         -0.0896705

20    4    0    4         -0.0942609

21    4    0    4         -0.0969748

22    2    0    5         -0.1078723

23    4    0    3         -0.1170983

24    4    0    5         -0.1272188

25    5    0    4         -0.1312145

26    5    0    4         -0.1360823

27    5    0    5         -0.1466995

28    5    0    5         -0.1510106

29    5    0    6         -0.1687743

30    5    0    5         -0.1742719

31    6    0    4         -0.1763605

32    6    0    3         -0.1944528

33    7    0    1         -0.1976362

34    4    0    4         -0.2005497

35    5    0    5         -0.2070544

36    4    0    4         -0.2116284

37    5    0    4         -0.2169469

38    2    0    5         -0.2182420

39    3    0    4         -0.2207537

40    3    0    3         -0.2233979

41    3    0    6         -0.2254453

42    4    0    3         -0.2272445

43    3    0    5         -0.2386275

44    2    0    5         -0.2407462

45    2    0    5         -0.2421679

46    4    0    4         -0.2439944

47    5    0    6         -0.2470364

48    2    0    8         -0.2550913

49    7    0    2         -0.2557325

50    6    0    3         -0.2612426

___________________________________________

Table 3. The measure of convergences , ,   and           in the function of m. Here m  is the number of eigenfunctions used in the summation.

__________________________________________________________________________________

m

__________________________________________________________________________________

1.00000     18.89260      0.46309      0.37880      0.10781

2.00000     11.76644      0.07931      0.37863      0.10781

3.00000      5.24199      0.07808      0.08113      0.10781

4.00000      5.22797      0.07802      0.08035      0.10771

5.00000      5.09352      0.06898      0.08031      0.10739

6.00000      5.05286      0.06896      0.07669      0.10732

7.00000      3.55927      0.06895      0.07667      0.03928

8.00000      2.87028      0.06890      0.04700      0.03847

9.00000      2.48959      0.05388      0.04438      0.03829

10.00000      2.36666      0.04941      0.04358      0.03796

11.00000      1.89116      0.02136      0.04323      0.03789

12.00000      1.64505      0.02051      0.03278      0.03768

13.00000      1.45780      0.01864      0.02382      0.03603

14.00000      1.00749      0.01862      0.02378      0.01219

15.00000      0.91779      0.01384      0.02376      0.01201

16.00000      0.66298      0.01383      0.01180      0.01201

17.00000      0.64758      0.01378      0.01178      0.01126

18.00000      0.64253      0.01378      0.01164      0.01112

19.00000      0.61875      0.01378      0.01163      0.00998

20.00000      0.61776      0.01378      0.01157      0.00997

21.00000      0.61914      0.01377      0.01131      0.00995

22.00000      0.54523      0.01376      0.01131      0.00516

23.00000      0.52314      0.01371      0.01015      0.00503

24.00000      0.48155      0.01200      0.01015      0.00502

25.00000      0.48035      0.01195      0.01014      0.00499

26.00000      0.48050      0.01190      0.01003      0.00499

27.00000      0.46324      0.01166      0.01002      0.00403

28.00000      0.41534      0.00990      0.01000      0.00400

29.00000      0.36303      0.00709      0.00988      0.00398

30.00000      0.32434      0.00700      0.00826      0.00387

31.00000      0.31665      0.00700      0.00802      0.00370

32.00000      0.29962      0.00697      0.00734      0.00370

33.00000      0.29815      0.00696      0.00733      0.00363

34.00000      0.29762      0.00695      0.00731      0.00362

35.00000      0.29308      0.00684      0.00729      0.00362

36.00000      0.29182      0.00679      0.00729      0.00362

37.00000      0.28869      0.00679      0.00710      0.00362

38.00000      0.28152      0.00678      0.00682      0.00362

39.00000      0.26967      0.00669      0.00628      0.00358

40.00000      0.26897      0.00667      0.00614      0.00357

41.00000      0.26538      0.00667      0.00595      0.00355

42.00000      0.25762      0.00667      0.00594      0.00290

43.00000      0.25394      0.00666      0.00586      0.00289

44.00000      0.25081      0.00653      0.00586      0.00285

45.00000      0.24817      0.00639      0.00585      0.00285

46.00000      0.24583      0.00637      0.00581      0.00284

47.00000      0.24397      0.00620      0.00581      0.00283

48.00000      0.23819      0.00613      0.00571      0.00274

49.00000      0.23634      0.00613      0.00564      0.00274

50.00000      0.23593      0.00613      0.00564      0.00271

__________________________________________________________________________________

Figure 1. The upper and side views of the structures obtained by the relations of Eq. (12).

The numbers of the figures means how many eigenfunctions  (m)  of the Laplacian are used

in the summations.

Results and conclusions

The greatest absolute values are   ,   and   in Table 1. They are the coefficients of the three bi-lobal eigenvectors (see Table 2. ).  If  the number of eigenfunctions ( m) in Eq. (12) is smaller than 7 ( the value k of the third bi-lobal eigenfunction ), the picture of the structure can be described as a planar or a curved two dimensional surface (Figure 1. ).  The eigenvectors ,  and  are 4, 4 and 5 –lobal but they have relatively small weight in Z (see Table 1.)  Although the eigenvectors , , ,  and  have relatively small weight in Z  and their lobality is from 3 to 5 they are important in eliminating the spiky features at the tube ends (Figure 1. )

We can obtain three dimensional surface only if m is greater than the order number of any bi-lobal eigenfunction.  The eigenvectors  and  have significant weight in Z, and its influence can be seen in Figure 1.  If  m is greater than 16 , practically there are not significant changing in the picture of the structure. Table 3. describes in a quantitative way the convergence of the structure.  For m=7 if all of the bi-lobal eigenfunctions are used, the average difference between the position of the atoms in the calculated and the converged structure () is 3.59Å. For m=16 this distance changes to 0.66 Å.

We have investigated altogether 11 junctions and we obtained three-dimensional structures only if all the three bi-lobal eigenfunctions were included in the summations. We had to take into consideration some other eigenvectors for eliminating the spiky behaviours at the end of the tubes. We have found in each cases a value for m which gave satisfactory coordinates that can be used for initial coordinates in a molecular mechanics calculations.

References

1. P. R. Bandaru, C. Dario, S. Jin and A. M. Rao,  Nature Mater. 4, 663 (2005).

2.  L. A. Chernozatonskii, Phys. Lett. A 172 (1992) 173-176.

3.  L. Chico, V. H. Crespi, L. X. Benedict, S. G. Louie, M. L. Cohen,

Phys. Rev. Lett. 76  (1996)  971-974.

4 . M. Menon, D. Srivastava, Phys. Rev. Lett. 79 (1997) 4453-4456.

5.  V. H. Crespi, Phys. Rev. B 58 (1998) 12671-12671.

6.  G. Treboux, P. Lapstun, K. Silverbrook, Chem. Phys. Lett. 306 (1999) 402-406.

7.   S. Melchor, N. V. Khokhriakov and S. S. Savinskii, Mol. Eng. 8 (1999)  315-344.

8.   A. N. Andriotis, M. Menon, D. Srivastava, L. Chernozatonkii,

Appl. Phys. Lett. 79 (2001)  266-268.

9.   A. N. Andriotis, M. Menon, D. Srivastava, L. Chernozatonkii,

Phys. Rev. Lett. 87 (2001) 066802 1-4.

10.  A. N. Andriotis, M. Menon, D. Srivastava, L. Chernozatonkii,

Phys. Rev. B 65   (2002) 165416 1-12.

11.  M. Terrones, F. Banhart, N. Grobert, J.-C. Charlier, H. Terrones, P. M. Ajayan,

Phys. Rev. Lett. 89 (2002).  75505 1-4.

12.  V. Meunier, M. B. Nardelli, J. Bernholc, T. Zacharia, J.-C. Charlier,

Appl. Phys. Lett. 81 (2002) 5234-5234.

13.  E. C. Kirby,

MATCH-Commun. in Math. and in Comp. Chem. 48 (2003) 179-188.

14.  S. Melchor, J. A. Dobado, J. of Chem. Inf. and Comput. Sci. 44 (2004) 1639-1646.

15.  M. Yoon, S. Han, G. Kimm, S. B. Lee, S. Berber, E. Osawa, J. Ihm, M. Terrones, F.

Banhart, J.-C. Charlier, N. Grobert, H. Terrones, P. M. Ajayan, D. Tomanek,

Phys. Rev.   Lett.   92 (2004) 75504 1-4.

16. I. Zsoldos, Gy. Kakuk, T. Réti, A. Szász, Modeling and Simul in Mat. Sci. and  Eng. 12, 1251 (2004).

17. I. Zsoldos, Gy. Kakuk, J. Janik, L. Pék, Diam.  Relat. Mater 14, 763  (2005).

18. I. László, A possible topological arrangement of carbon atoms at nanotube junctions,

Fullerenes, Nanotubes and Carbon Nanostructures  13, 535 (2005).

19. I. László, Topological description and construction of single wall carbon nanotube junctions, Croat. Chem. Acta  78, 217 (2005).

20. I. László, Construction of carbon  nanotube junctions,

Croat. Chem. Acta  xx, xxx (2007).

21.  I. László, Construction of atomic arrangement for carbon nanotube junction,

Phys. Stat. Sol. (b)  244, 4265,  (2007).

22. D.E. Manolopoulos, P.W. Fowler, Molecular graphs, point groups and fullerenes,

J. Chem. Phys. 96, 7603, (1992).

23. T. Pisanski, J.S. Shawe-Taylor, Characterising graph drawing with eigenvectors,

J. Chem. Inf. Comput. Sci., 40, 567, (2000).

24. P. W. Fowler, D.E. Manolopoulos,   An Atlas of Fullerenes, Oxford University Press, Oxford,    (1995).

25. P. W. Fowler, T. Pisanski, J. Shawe-Taylor, Molecular graph eigenvectors for molecular coordinates, in Graph Drawing, DIMACS International Workshop, R. Tamassia and I. G. Tollis (Eds.),  GD’94 Princeton, New Jersey, USA, October 10-12, 1994, pages 282-285.

26. I. László, A. Rassat, P.W.  Fowler, A.  Graovac, Topological coordinates for toroidal

structures,  Chem. Phys. Lett. 342, 369 (2001).

27. I. László, Topological coordinates for nanotubes,  Carbon 42, 983 (2004).

28. A. Graovac, D. Plavsic, M. Kaufman, T. Pisanski, E.C. Kirby, Application of the adjacency

matrix eigenvectors method to geometry determination of toroidal carbon molecules,

J. of Chem. Phys. 113, 1925  (2000).

29. I. László, A. Rassat,  The geometric structure of deformed nanotubes and the topological

coordinates, J. Chem. Inf. Comput. Sci. 43, 519 (2003).

30. I. László, The electronic structure of nanotubes and the topological arrangements of carbon

atoms,  in Frontiers of Multifunctional Integrated Nanosystems, Buzaneva, E., Scharff, P.

(Eds.), NATO Science Series, II. Mathematics, Physics and Chemistry, 152, 11, (2004).

31. I. László, Topological coordinates for Schlegel diagrams of fullerenes and other planar

graphs,   in Nanostructures: Novel Architecture, Diudea, M.V. (Ed.), Nova Science

Publishers, Inc. ,New York,  page 193 (2005).

32. M.S. Dresselhaus, G. Dresselhaus and P.C. Eklund,   Science of fullerenes and carbon nanotubes, Academic Press, San Diego, Boston, New York, (1996).

# Text boxes

5

4

3

6

7

8

9

10

11

12

13

14

15

16

50

1165